## Slide 1: RESEARCH AND DEVELOPMENT OF HETEROJUNCTION BASED PHOTODETECTOR
MID SEMESTER EVALUATION
Presented by
Anand Nivrutti Kachale
M.S. Research, IIT Indore
Supervised by
Dr. Vipul Singh
Professor, IIT Indore
Molecular and Nanoelectronics Research Group
Department of Electrical Engineering
Indian Institute of Technology Indore

## Slide 2
OUTLINE
Motivation
Introduction
Objective
Proposed work
  ZnO Nanostructure growth
  SEM and UV-Vis. result analysis
  LSPR and Ag NPs deposition mechanism
  Ag NPs deposition
  SEM and UV-Vis. result analysis
  COMSOL simulation for PVT
Conclusion
Plan of action
Acknowledgements
References

## Slide 3
Increase in demand of photodetectors
[1]
[2]
MOTIVATION

## Slide 4
Phototransistor
Photoconductor
Photodiode
[3]
[4]
[5]
PHOTODETECTORS
INTRODUCTION

## Slide 5
Organic - Organic
HETEROJUNCTION TYPES
Inorganic - Inorganic
Organic - Inorganic (Hybrid)
Phthalocyanine/C60
C60
[8]
ZnO/Co3O4
ZnO/P3HT
[9]
[10]

## Slide 6
DEVICE PARAMETERS
Metric | Definition | Unit
Rectification ratio |  | --
Responsivity (R) |  | AW-1
Photosensitivity (S) |  | --
Specific Detectivity (D*) |  | Jones
[8]
[9]

## Slide 7
OBJECTIVES
Fabrication of heterojunction photodetector using solution process.
  Optimization of various parameters to obtain crystalline growth of ZnO nanorods.
  Study effect of UV-irradiation time and AgNO3:Ethanol conc. on Ag particle size deposited.
To study physical vapor transport technique and perform simulation to get optimized parameters.
Fabrication of heterojunction photodetector using physical vapor transport technique.

## Slide 8
NANOSTRUCTURE GROWTH
Spin coating @ 3000rpm for 30 sec
Annealing at 240⁰ for 5 mins
Hydrothermal growth for 0-10mM KMnO4 for 3hrs
ZnO Nanorods growth
Glass
ZnO Seed layer
ZnO Nanorods
ZnO Seed solution 3M

## Slide 9
3M ZnO Seed
Pristine
0.5mM KMnO4
1mM KMnO4
5mM KMnO4
10mM KMnO4
UV-Vis.
Characterization
SEM
Characterization
NANOSTRUCTURE GROWTH
Hydrothermal growth
ZnNO3+HMTA

## Slide 10
SEM RESULTS
Pristine
1mM
0.5mM
5mM
10mM
1mM
Inverted

## Slide 11
UV-VIS RESULTS
Sample Details | Bandgap (eV)
Pristine | 3.29
0.5mM KMnO4 | 3.27
1mM KMnO4 | 3.26
10mM KMnO4 | 3.2

## Slide 12
PCR (PHOTO CHEMICAL REDUCTION)
Drop casted the prepared solution on the nanostructure
Rinse in DI
Ag NP deposited ZnO Nanorods
Preparation of AgNO3 : Ethanol solution of various concentrations
Ethanol solution
AgNO3 solution
UV irradiation for 5 sec
Black box

## Slide 13
[15]
Localized Surface Plasmonic Resonance
AgOx
W
Ag
ZnO
e-
LSPR
Incident radiation
e- e-
LSPR effect
Ag NPs deposition mechanism
UV irradiation
CH3CH2OH
ZnO
e- e- e-
h+ h+ h+
Ag+
ZnO
Ag
ZnO
Ag Nuclei
Ag NPs
Ag
CH3CHO

## Slide 14
3M ZnO Seed
0.5mM KMnO4
1mM KMnO4
1mM INV KMnO4
Hydrothermal growth
ZnNO3+HMTA
UV irradiation for 5 sec
AgNO3 : Ethanol
No irradiation
1:9
1:4
3:7
UV-Vis.
Characterization
SEM
Characterization
Ag NP DEPOSITION
Additive

## Slide 15
SEM RESULTS 0.5mM KMnO4 with Ag NPs
1:9
AgNO3 : Ethanol
No irradiation
1:4
AgNO3 : Ethanol
3:7
AgNO3 : Ethanol

## Slide 16
SEM RESULTS 1mM KMnO4 with Ag NPs
1:9
AgNO3 : Ethanol
No irradiation
1:4
AgNO3 : Ethanol
3:7
AgNO3 : Ethanol
Increased diameter of ZnO nanorods
Increased growth rate of Ag NPs

## Slide 17
UV-VIS RESULTS
0.5mM KMnO4
1mM KMnO4
Higher shift in resonant wavelength with higher conc. of AgNO3

## Slide 18
UV-VIS RESULTS
0.5mM KMnO4
1mM KMnO4
Higher shift in resonant wavelength with higher conc. of AgNO3

## Slide 19
Physical Vapour Transport
[12]
PVT schematic
Laminar flow
Heat transfer
MULTIPHYSICS STUDY
+

## Slide 20
COMSOL SIMULATION
Velocity profile
Temperature profile
Geometry
U0 = 15 cm/s
P0 = 0 Pa
Defined boundary walls
U = 0 cm/s
T0 = tn … n = 1 to 12

## Slide 21
CONCLUSION
Synthesized ZnO nanorods using various concentrations of KMnO4 additive.
With increase conc. of KMnO4 increase in diameter of nanorods and lower shift in bandgap energy is observed.
With increase in AgNO3:Ethanol conc. the Ag NPs density and growth rate increases also on larger diameter nanorods growth rate and hence density is higher.
For increasing conc. of AgNO3:Ethanol the resonant wavelength is observed to have a higher shift.
Temperature variation profile due to the gas flow in PVT tube is studied in COMSOL.

## Slide 22
PLAN OF ACTION
Work | Sem1 |  | Sem2 |  | Sem3 |  | Sem4 | 
 | Q1 | Q2 | Q3 | Q4 | Q5 | Q6 | Q7 | Q8
Experimental training and literature review about proposed topic |  |  |  |  |  |  |  | 
Simulation |  |  |  |  |  |  |  | 
Fabrication experiments |  |  |  |  |  |  |  | 
Device fabrication and optimization |  |  |  |  |  |  |  | 
Paper Writing |  |  |  |  |  |  |  | 
Thesis Writing |  |  |  |  |  |  |  | 

## Slide 23
My sincere thanks to:
My thesis supervisor “Dr. Vipul Singh” for his help and guidance.
I would like to extend my gratitude to my PSPC members, Dr. Eswara Prasad Korimilli and Dr. Swaminathan Ramabadran.
I am grateful to IIT Indore for providing the necessary resources for research.
I would also like to thank my team and colleagues for technical discussions.
I am thankful towards MHRD for providing for teaching assistantship.
ACKNOWLEDGEMENTS

## Slide 24
[1] Shan, T., Hou, X., Yin, X. et al. Organic photodiodes: device engineering and applications. Front. Optoelectron. 15, 49 (2022)
[2] Zhuge, Fuwei, et al. "Nanostructured materials and architectures for advanced infrared photodetection." Advanced Materials Technologies 2.8 (2017): 1700005.
[3] Phillips, J., et al. "Electronic and optoelectronic devices based on semiconducting zinc oxide." (2011): 101-127.
[4] M. R. Shenoy [NPTEL] “Semiconductor Optoelectronics, IIT Delhi” (Part IV-4)
[5] Xu, Hua, et al. "High responsivity and gate tunable graphene‐MoS2 hybrid phototransistor." Small 10.11 (2014): 2300-2306.
[6] Parasuraman S. [NPTEL] “Fundamentals of electronic materials and devices, IIT Madras”(Week 7.4)
[7] Plakhotnyuk, Maksym. "Nanostructured Heterojunction Crystalline Silicon Solar Cells with Transition Metal Oxide Carrier Selective Contacts." (2018).
[8] Zhang, Xiaoqiang, et al. "All-organic flexible heterojunction thin film photodetectors based on phthalocyanines/C60." AIP Advances 12.8 (2022).
REFERENCES

## Slide 25
REFERENCES
[9] Rana, Amit Kumar, et al. "Transparent Co3O4/ZnO photovoltaic broadband photodetector." Materials Science in Semiconductor Processing 117 (2020): 105192.
[10] Agrawal Jitesh, et al. "ZnO/Pt/P3HT hetero-junction configuration for high performance Self-biased UV Detection." IEEE Electron Device Letters (2023).
[11] Ren, H., Chen, J.-D., Li, Y.-Q., Tang, J.-X., Recent Progress in Organic Photodetectors and their Applications. Adv. Sci. 2021, 8, 2002418. https://doi.org/10.1002/advs.202002418
[12] Reese, Colin, and Zhenan Bao. "Organic single-crystal field-effect transistors." Materials Today 10.3 (2007): 20-27.
[13] Zhao, Xiaotong, et al. "Organic Semiconductor Single Crystal Arrays: Preparation and Applications." Advanced Science (2023): 2300483.
[14] Laudise, R. A., et al. "Physical vapor growth of organic semiconductors." Journal of crystal growth 187.3-4 (1998): 449-454.
[15] Zhang, Yifan, et al. "Radiation induced plasmonic nanobubbles: fundamentals, applications and prospects." AIMS Energy 9.4 (2021): 676-713.

## Slide 26
THANK YOU !